## Slide 1
DIMENSIONS OF STRENGTH
Modulus of Elasticity
Bending Strength
Density
Chart: FORMULATION V MATERIAL TYPE
| Wood Like | WoodComposite | Composite | Concrete Composite | Concrete Board
Resin | 10 | 10 | 10 | 10 | 10
Biomass | 90 | 50 | 30 | 20 | 10
Paper | 0 | 30 | 50 | 40 | 40
Ash | 0 | 10 | 10 | 20 | 40
Y axis - composition (I think - Elena)
Notes: More ash you add the more concrete like. More biomass the more wood like. More paper the more of a composite.

## Slide 2
Chart: FIRE RESISTANCE V MATERIAL FORMULATION
| D | C | B | A2 | A1
WOOD | 100 | 0 | 0 | 0 | 0
WOOD COMPOSITE | 2.4 | 4.4 | 1.8 | 2.8 | 0
COMPOSITE | 2 | 2 | 3 | 5 | 0
CONCRETE COMPOSITE | 20
CONCRETE BOARD | 0 | 0 | 0 | 0 | 100

Notes: Gareth is interested in the middle area where a new formulation could give better fire protection than expected (map existing commercial products to their respective categories.